# SNOL 8,2/1100 LHM21

SNOL 8.2/1100 ashing furnace with vacuum-formed ceramic fiber chamber is designed for ashing and burn-off processes up to 1100°C. Fan-assisted chimney permits the elimination of smokes from the chamber during the process.

#### BASIC MODEL

- One piece high thermal efficiency vacuum-formed ceramic fiber chamber;

- Heating elements are embedded in vacuum-formed fiber in four sides around a chamber;

- Fan-assisted chimney for smoke and humidity extraction;

- Continuous air change in the chamber;

- Door opens upwards;

- Door safety switch;

- Microprocessor – controlled thermoregulator;

- Outside casing – metal sheet, powder painting grey;

- High quality, ecological thermal insulation material;

- Low electric power consumption;

- Short heating up/cooling down period;

- High degree of accuracy;

- 1 year guarantee.

#### OPTIONS

- Process observation window (o 35 mm) up to 1100 °C;

- Additional ceramic hearth plates;

- Buzzer;

- Protection against overheating;

- Data recorder;

- RS232/RS-485/USB interface;

- Calibration of temperature measurement system;

- Additional 1 year guarantee.

## Specification

| Technical data | Dimensions | SNOL 8,2/1100 LHM21 |
| --- | --- | --- |
| Useful volume | Liters | 8,2 |
| Rated power not more than | kW | 1.8 |
| Rated supply voltage | V | 230 |
| Rated frequency | Hz | 50 |
| Number of phases | - | 1 |
| Continuous operating temperature | °C | T+10-1100 |
| Maximum temperature | °C | 1100 |
| Working chamber material | - | Fiber muffle |
| Maximum heating- up time (without charge) | Min. | 50 |
| Temperature stability in working chamber at rated temperature in thermal steady state without charge not more than | ± °C | 1 |
| Temperature uniformity in working space at rated temperature in thermal steady state without charge not more than | ±°C | 10 |
| Furnace working chamber dimensions: |
| width | mm | 195 |
| depth | mm | 310 |
| height | mm | 135 |
| Furnace external dimensions: |
| width | mm | 445 |
| depth | mm | 710 |
| height | mm | 495* |
| Mass | kg | 28 |

* – should increase by 20-85 mm, depending on the chimney